## Slide 1: Module-4(b) Thermal Expansion of solid material
Aim:
To study the thermal expansion behavior of solid materials using a dial gauge dilatometer.
ESO205: Nature and Properties of Materials
By- Pragya Dixit, Research Scholar

## Slide 2
0
r0
(Interatomic distance)
r
r1'
r2'
r2"
r1”
r1
r2
Repulsion Energy
Attraction Energy
Total Energy
T1
T2>T1
(Energy)
Figure: Potential energy Vs Interatomic distance
(B/rn )
(A/rm )
Total potential energy
V(r) =( - (A/rm ) + (B/rn ))
Decreasing r lowers the energy
Theory:

## Slide 3
Asymmetric shape of the potential energy curve can be noticed.
Degree of asymmetry is a function of the values of the exponent of m and n in equation.
m<n
In ionic crystals, m ~1 and n ~ 12, here m = 1 corresponds to coulomb attraction between two point charges.
In molecular crystals, m ~ 6.
At temperature T1 and energy E1, the r oscillates from r 1‘ to r 1“.
r 1 = (r 1‘ + r 1“)/2
At temperature T2 > T1 and energy E2 , r oscillates from r 2‘ to r 2“.
r2 = (r 2‘ + r 2“)/2
At T2, r2>r1 leads to thermal expansion.

## Slide 4
Asymmetric shape of the potential energy curve (due to anharmonic nature of the lattice vibrations) is responsible for the thermal expansion.
Large binding energy high melting point of a material
Have a deep potential energy minimum
At T<<<Tm, asymmetry of the curve exist only to a small extent.
A material with a high melting point (T ° K) would, near room T shows low thermal expansion.

## Slide 5
Isotropic materials (ex: metals, glass, plastics ):
Exhibit the same thermal expansion in all directions.
Non isotropic crystals (ex: wood, composites):
Possess different Th. Exp. values in various directions.
Poly crystalline specimen (ex: ceramics, ice) :
Has randomly oriented non isotropic crystals so possess avg of expansion coefficient of all the directions.
Multiphase material (ex: Steels, composites)
Has weighted average of the expansion coefficients of its component phases.
Thermal expansion coefficient can be measured by knowing two physical quantities:
Displacement
Temperature

## Slide 6: Objective To study the thermal Expansion behaviour of solid material using a dial gauge dilatometer
Apparatus
Fused silica tube
Dial gauge dilatometer
Vertical Tube Furnace
Variac (Auto transformer) for power supply
Temperature Controller
Potentiometer
K-type Thermocouple (Chromel-Alumel) and
Specimen (Aluminium), Fireclay bricks
Dial gauge (mechanical magnification)

## Slide 7: Experimental Setup
Dial Gauge
Thermocouple
Milli voltmeter
Variac
Vertical tube Furnace
Specimen tube

## Slide 8: Schematic Diagram & Dilatometer Assembly Experimental Setup
Dial Gauge
Fused Silica Tube
Fused Silica Rod
Heat Transfer Fluid
Specimen
Alumina tube
Bottom End closed
Specimen
Dial gauge
Tighten with clamp
Nut bolt tighten with Inconel plate
Fused Silica Rod
Fused Silica Tube
(Least count=0.001mm)

## Slide 9: Internal Experimental Design
Specimen( Aluminium )
Outer Tube
Outer tube
Inner tube
Specimen
Inner tube
Silica Tubes

## Slide 10: Methodology
Take pure aluminium (why Al?)
Mount one of the samples at the bottom of the quartz tube which is closed at one end
Place the quartz tube on the top of specimen
Attach the dial gauge on the top of outer quartz tube by Inconel clamp
Insert the whole assembly in tube furnace
Read the dial gauge reading at different temperature

## Slide 11: Linear thermal expansion coefficient
Change in length of a rod due to thermal expansion.
The change in length with temperature for solid material can be expressed as follows:
Or
α*△T = (Lf -Lo)/Lo
α = (△L)/( △T *Lo )
Lo and Lf are the initial and final length (after heat treatment), respectively.
α is linear thermal expansion coefficient.
△T= Tf -To

## Slide 12
1. Show one adverse effect of differential dilatation (thermal expansion mismatch). Check out your surrounding if you can find any such example (Don’t forget to post a picture of whatever you have observed with proper explanation).
Question:
Thank You